#### ПОКАЗАТЕЛИ КАЧЕСТВА

СОРТ: 	F2040

ДАТА: 	Май 2010

НАЗНАЧЕНИЕ и ОСОБЕННОСТИ:	Обеззоленные фильтры для количественных анализов

со средне-медленной скоростью фильтрации

ФАСОВКА: 	100 шт фильтров-листов в индивидуальной упаковке

##### РАЗМЕР: 	- Круглые:  21, 25, 42,5, 47, 50, 55, 70, 90, 100, 110, 125, 150, 185, 240, 270, 320  мм, (

- Листы: 580x580 мм

Партия фильтровальной бумаги обозначается шестью цифрами.

ТЕХНИЧЕСКИЕ ТРЕБОВАНИЯ:

Масса 1 м2  (по ISO 536): 	84 г/м2

Толщина: 	0,170 мм

Фильтрующая способность: 	100 сек

Скорость фильтрации: 	Средняя, ближе к Медленной

Размер пор: 	7 - 9 мкм

Сопротивление продавливанию во влажном состоянии  (по ISO 2758): 	>30 кПа

Золы содержание  (по DIN 54370): 	<0,007%

#### ***********************************************************************************************

#### TECHNICAL DATA SHEET

GRADE: 	F2040

DATE: 	May 2010

NAME:	Quantitative filter paper

PACKAGING: 	Boxes of 100 units

##### FORMAT: 	- Circles:  21, 25, 42,5, 47, 50, 55, 70, 90, 100, 110, 125, 150, 185, 240, 270, 320  mm. (

- Sheets: 580x580 mm.

TRAZABILITY: 	- Batch: 6 digits

TECHNICAL SPECIFICATIONS:

Basis weight (ISO 536): 	84 gr./m2.

Thickness: 	0,170 mm.

Filtration time for distilled water: 	100 s

Filtration: 	Medium Slow

Retention: 	7 - 9 (m

Wet bursting strength (ISO 2758): 	>30 kPa

Ash content (DIN 54370): 	<0,007%

Features: Medium Slow speed filtration quantitative filter paper